## Slide 1
CdSe Quantum Dots
Core & Core/Shell Nanostructures
Comparing optical properties, surface passivation,
and quantum confinement behavior
Core
Shell
Ligands
Semiconductor Nanomaterials | Photophysics & Surface Chemistry

## Slide 2
CdSe Core-Only Quantum Dots
Bare semiconductor nanocrystals — simple structure, inherent limitations
CdSe
Core
Surface trap states (dangling bonds)
◈
Quantum Confinement
Strong size-tunable bandgap from ~1.8 eV (bulk) to >2.5 eV; emission wavelength 490–650 nm controlled by crystal diameter.
◈
Surface Traps
Unsaturated Cd²⁺ / Se²⁻ dangling bonds at the surface act as non-radiative recombination centers, reducing PLQY (<20 %).
◈
Photostability
Susceptible to photo-oxidation and photobrightening; emission intermittency (blinking) is pronounced due to trap-mediated Auger processes.
◈
Organic Ligands
Capped with TOPO, oleic acid, or amines to provide colloidal stability, but ligand exchange is facile and can worsen trapping.
Typical PLQY: 5 – 20 %
Emission FWHM: ~30–50 nm

## Slide 3
CdSe/ZnS Core/Shell Quantum Dots
Epitaxial ZnS shell passivates surface traps → dramatically enhanced optical performance
CdSe
ZnS
Shell layer
(1–3 monolayers)
Surface Passivation
ZnS shell (wider bandgap, ~3.5 eV) confines carriers within the CdSe core, eliminating dangling-bond trap states and suppressing non-radiative recombination.
Quantum Yield & Brightness
PLQY jumps to 50–90 %+, with narrow emission linewidth (~20–25 nm FWHM). Near-unity efficiencies achieved with multishell (CdSe/CdS/ZnS) architectures.
Photostability
Dramatically reduced blinking and photo-oxidation. The shell acts as a physical barrier against oxygen and solvent quenching, extending fluorescence lifetime.
Band Alignment
Type-I alignment: both electron and hole wave functions are confined to the CdSe core; ZnS provides a high tunnel barrier (~0.9 eV valence, ~1.1 eV conduction offset).
PLQY: 50–90 % FWHM: ~20–25 nm Lifetime: 20–40 ns vs Core-only ~5–10 ns, <20 % QY